Test Report

Report No. Rev

Date Reported Job No.

Date Received

:	K25-20171_3

:	0

:	30/09/2025	Reviewed By	Approved By

:	K25-20171	Nuwan Mathews	Rodelio Lagunilla CTTA#0705,

:	03/09/2025	CTTA#0913	For and on behalf of Element Saudi Arabia Company Limited

| Client Name | : | ULO System Saudi Arabia |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Client Address | : | Saudi Arabia |  |  |  |
| Project Name | : | 1657-B & E-12-2024-Al Gihaz |  |  |  |
| Project No. / Location | : | 1657-B & E-12-2024-Al Gih |  |  |  |
| Project Owner | : | SAUDI ARAMCO |  |  |  |
| Consultant | : | Saudi Aramco |  |  |  |
| Contractor | : | Al Gihaz |  |  |  |
| Mix Grade | : | C40 Mpa, Type V Cement |  |  |  |
| Pour Location | : | Free Span Correction |  |  |  |
| Compressive Strength |  | ASTM C109/C109M : -20b |  |  |  |
| Test Facility | : | Dammam | Batching Date/Time | : | 12/08/2025 |
| Sampling Certificate | : | N/A | Sampling Date/Time | : | 12/08/2025 |
| Sampling Method | : | ASTM-C-109/109M-20b | Time of Making Cubes | : | 12/08/2025 |
| Compaction Method | : | Hand-Using Compacting Bar | Cube Manufactured By | : | Gaokaran |
| Volume Determination | : | ASTM C-109/C109M-20b | Place of Making Cubes | : | Site |
| Air Content (%) | : | N/A | Supplier | : | N/A |
| Site Curing | : | Site Conditions | Cube Delivered By | : | Client |
| Laboratory Curing | : | Moist 23.0 ± 2.0°C | Dimensions | : | Checked Nominal |
| Removal of Fins | : | Manual - using steel file | Nominal Size (mm) | : | 50x50x50 |
| Sampling Location | : | Dammam | Flow/Slump (mm) | : | N/A |

Test Results

Element Saudi Arabia Company Limited	T: +966 (0) 13 812 7750 Dammam 2nd Industrial City - Cross Section 76 & 27 info.saudiarabia@element.com PO Box 31775, Al Khobar 31952	element.com

Dammam, Kingdom of Saudi Arabia

| Client Ref. | Our Sample No. | Req. Test Age (Days) | Age at Test (Days) | Date Tested | Cond. Upon Receipt | Cond. at Test | Dimensions (mm) |  |  | Mass in air (Kg) | Density (kg/m3) | Maximum Failure Load (kN) | Comp. Strength (N/mm2) | Type of Fracture |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | L | W | H |  |  |  |  |  |
| SC9-FS54 | 1 | 28 | 28 | 09/09/2025 | N | SSD | 50 | 50 | 50 | 0.241 | 1930 | 150.2 | 60.1 | SF |
| SC9-FS54 | 2 | 28 | 28 | 09/09/2025 | N | SSD | 50 | 50 | 50 | 0.243 | 1940 | 145.5 | 58.2 | SF |
| SC12-FS55A | 3 | 28 | 28 | 09/09/2025 | N | SSD | 50 | 50 | 50 | 0.241 | 1930 | 152.1 | 60.8 | SF |
| SC12-FS55A | 4 | 28 | 28 | 09/09/2025 | N | SSD | 50 | 50 | 50 | 0.244 | 1950 | 146.3 | 58.5 | SF |
| SC14-FS72 | 5 | 28 | 28 | 09/09/2025 | N | SSD | 50 | 50 | 50 | 0.240 | 1920 | 171.7 | 68.7 | SF |
| SC14-FS72 | 6 | 28 | 28 | 09/09/2025 | N | SSD | 50 | 50 | 50 | 0.243 | 1940 | 178.4 | 71.4 | SF |
| Average Compressive Strength (N/mm²) |  |  |  |  |  |  |  |  |  |  |  |  | 63.0 |  |

Legend: SF - Satisfactory, N - Normal, SD - Saturated, SSD - Saturated Surface Dry

Notes:  Unless marked with *, dimensions of cylinder were within 1% of nominal size.

Curing before delivery to lab was performed outside the control of the test laboratory.

If condition at test denoted as moist, mass and density determined in as received state, otherwise is saturated state.